Enhancement of Cancer Cellular Uptake by the Morphology of Lipid-Based Nanodiscs

Wafa Aresh1, Ying Liu2, Jessica Sine3, Derek Thayer3, Anu Puri3, Yike Huang4, Yong Wang4, and Mu-Ping Nieh1,2,5*

1Department of Biomedical Engineering, University of Connecticut, Storrs, CT, USA

2Department of Chemical & Biomolecular Engineering, University of Connecticut, Storrs, CT, USA

3Basic Research Laboratory, Center for Cancer Research, National Cancer Institute, Frederick, MD, USA

4Department of Biomedical Engineering, Pennsylvania State University, University Park, PA, USA

5Polymer Program, Institute of Materials Science, University of Connecticut, Storrs, CT, USA

Abstract

The interaction between cells and particles is recently found morphologically and material dependent. In many cases, “spheres” may not be the best candidates for cellular uptake. In this study, self-assembled nanodiscs and nano- oblate vesicles composed of a zwitterionic long-chain 1,2-dihexadecanoyl-sn-3-phosphocholine (DPPC), a zwitterionic short chain1,2-dihexanoyl-sn-glycero-3-phosphocholine (DHPC) doped with small quantities of charged long-chain 1,2-dihexahecanoyl-sn-glycero-3-phospho-(1’-rac-glycerol) (DPPG) and a PEGylated lipid, 1,2-distearoyl-sn-glycero-3-phosphoethanolamine-N-[methoxy(polyethylene glycol)-2000] (DSPE-PEG2000) were synthesized at the same composition. Both morphologies are uniform and have similar sizes. Small angle neutron scattering data show that the average diameter and thickness of the nanodiscs are 21.0 and 5.4 nm, respectively, and that the outer long- and short- axes of the oblate vesicle yield 34.2 and 12.0 nm, respectively. The cellular uptake of these two types of Nilered-containing nanoparticles was investigated as incubated with the lymphoblast cancer cells (CCRF-CEM) at 37 oC for 2 hours. The result indicates that the cellular uptake of nanodiscs is 3 ~ 5 fold of that of the nanovesicles. Moreover, the fact that the locations of nanoparticles are different in the cells suggests a morphological dependence of cellular uptake mechanism.