Intensification of breaking of water-in -oil emulsions by membranes, treated in the area of corona discharge or in the plasma flow

Dryahlov V.О, Shaihiev Т.I., Shaihiev I.G., Galihanov М.F., Bonev B.S.

The Kazan National Research Technological University

Water-in-oil emulsions (WOE) are formed as a result of petroleum processing and utilizing of oil products in the enterprises of chemical and petrochemical profile all over the world at the rate of more millions t/year. WOE form the aggressive stable multicomponent structure which contains surfactant species (SS) and different emulsifiers such as salts, asphaltens, gums, oil-soluble organic acids and minute impurities such as slime and clay.

In recent times ultrafiltration method is used for the breaking process of WOE. The main advantages of this method are: high efficiency, deficiency of existing reagents, small floor space for equipment, energy efficiency, and so the opportunity of close water cycle organizing. Disadvantage of membrane methods is the pollution of membrane surface by the dispersion phase of pollutant. As a result the slowdown of separating process occurs.

In view of the forgoing, high-powered membranes treatment is perspective for the purpose of ultrafiltration intensification of WOE with engineering and ecological side, particularly, in the field of corona discharge or in the flow of low temperature high frequency plasma of low pressure.

Research results of breaking of model WOE by polyacrylonitrile (PAN) membranes with the molecular weight cut-off (MWCO) 25 kDa are introduced in this work. These leaked particles were treated in the field of corona discharge or in the plasma flow. The treatment by the corona discharge was held under the next conditions: productive time (τ) was 0.5, 1, 1.5 min, electrode voltage (U) was 5, 10, 15 kV; plasma treatment was done in gas environments of argon and nitrogen, argon and air during (τ) – 1.5, 4, 7 min for anode voltage (U) - 1.5, 3.5, 5.5 and 7.5 кV.

Productivity and effectiveness are considered as the main parameters of membrane division of emulsion. The first factor is the ratio of quantity of passed flow though membrane of separating environment to production of the process life and area of the filter element, which is 1,73·10-3 м2  in this case. Effectiveness is determined by change of values of chemical oxygen demand (COD) before and after the process of emulsion division. This process was measured on the autotitrator «T70» of «Mettler Toledo» producer company . Results are introduced on the figures 1-3 and  in the Table 1, 2.

a)

b)

c)

Figure 1 –Productivity of emulsion breaking by PAN membranes with the MWCO 25 kDa, which are electret under the next conditions: a) U = 5 kV; b) U = 10 kV; c) U = 15 kV.

Curves analysis presented on the figure 1 shows the increase in productivity of modified PAN membranes with MWCO 25 kDa till 2 times. These leaked particles were treated in the field of corona discharge in all regimes of electro treatment (Figure 1a-c). In addition of the above the great value of the present parameter for each value U is observed when τ = 1,5 min, and the greatest value was registered when U = 5 кV.

Table 1 – received COD filtrates under division by electret PAN membranes with the MWCO 25 kDa.

| U, kV | COD, мg О2/l |  |  |
| --- | --- | --- | --- |
|  | Productive time, τ, min |  |  |
|  | 0,5 | 1 | 1,5 |
| 5 | 10002 | 7803 | 7639 |
| 10 | 6578 | 5642 | 6810 |
| 15 | 6812 | 6339 | 7462 |
| Unmodified membrane | 8520 |  |  |
| Emulsion | 166550 |  |  |

Presented values in the table 1 show improving effectiveness of emulsion breaking of modified PAN membranes with the MWCO 25 kDa in 8 cases from 9. The value of COD filtrate received by the use of unmodified membrane is 8520 мg О2/l, properly, efficiency factor is 95,0 %. The bottom value of COD filtrate is 5642 мg О2/l when using membrane electreted under U = 10 kV and τ = 1 min, the efficiency factor is 96,5 %.

a)

b)

c)

d)

Figure 2 – Productivity of emulsion breaking  by PAN membranes with the MWCO of leaked particles 25 kDa, treated in the plasma flow in gaseous medium of argon and nitrogen when the value of anode voltage is: a) Ua = 1,5 kV; b) Ua = 3,5 kV; c) Ua = 5,5 kV; d) Ua = 7,5 kV.

The previous revealed effect of increase in productivity of modified membranes in comparison with unmodified membrane as high as 2 times is registered (Figure 2) as a result of plasma treatment in argon and nitrogen medium of PАN membranes with the MWCO 25 kDa. In addition to above the immense increase of the present parameter was registered when U = 1,5 кV and τ = 4 and 7 min, Ua = 7,5 кV and τ = 7 min, in other cases  the increase was feebly marked.

a)

b)

c)

d)

Figure 3 – Productivity of emulsion breaking by PAN membranes with the MWCO 25 kDa, treated in the plasma flow in gaseous medium of argon  and air when the value of anode voltage is: a) Ua = 1,5 kV; b) Ua = 3,5 kV; c) Ua = 5,5 кV; d) Ua = 7,5 кV.

Plasma treatment in the argon and air medium of PАN membranes with the MWCO 25 kDa promotes the great increase in productivity by a factor of three in comparison with unmodified membrane. At that on all occassions the largest values of the present parameter are registered when treatment time τ = 4 min, and maximum is registered when U = 5,5 kV.

As follows from the analysis of facts presented in the table 2, it was found that plasma treatment of PАN membranes with the MWCO 25 kDa promoted values decrease of COD filtrates of modified filter elements, in this example in 58,3 % cases. Decrease of present parameter occured with increase of values U and τ in the case of plasma influence in argon with air medium. Analogous dependance was not determined for membranes subjected to plasma treatment in argon and nitrogen medium.

The least value COD = 4610 мg О2/l  was obtained when membrane using, treated in argon and air medium under Ua = 7,5 кV, τ = 7 min; values of COD filtrate, after division of unmodified membrane are 7050 mg О2/l, properly, the efficiency factor is 97 and 95 %.

Table 2 – received COD filtrates under breaking of emulsion by plasma treated PAN membranes with the MWCO 25 kDa

| Gaseous medium | Ua, кV | COD, мg О2/l |  |  |
| --- | --- | --- | --- | --- |
|  |  | Plasma treatment time, min |  |  |
|  |  | 1.5 | 4 | 7 |
| Argon+nitrogen 70 : 30 | 1.5 | 7717 | 6130 | 5530 |
|  | 3.5 | 5240 | 6630 | 7835 |
|  | 5.5 | 5660 | 6450 | 7290 |
|  | 7.5 | 6680 | 7330 | 10030 |
| Argon air 70 : 30 | 1.5 | 7340 | 6500 | 5730 |
|  | 3.5 | 8430 | 7710 | 7540 |
|  | 5.5 | 8290 | 6250 | 5740 |
|  | 7.5 | 5820 | 5130 | 4610 |
| Unmodified membrane |  | 7050 |  |  |
| Emulsion |  | 166550 |  |  |

This is the way how positive effect of corona discharge influence and plasma on PАN membranes for the purpose of increase in productivity and selectivity of WOE division was determined based on the results of the research conducted.