# The mobility vs. carrier density trend in wafer-scale epitaxial graphene on SiC, and how it can be defeated

C. Dimitrakopoulos,1 T. J. McArdle,2 D. Farmer,3 A. Grill,3 D. Pfeiffer,3 Ph. Avouris3

1. Chemical Engineering Dept. University of Massachusetts, Amherst, MA 01003.

2. IBM Microelectronics, E. Fishkill, NY 12533.

3. IBM Thomas J. Watson Research Center, Yorktown Heights, NY 10598.

Graphene’s unique and exceptional properties make it attractive for technological applications in many areas, including high-speed electronics. The establishment of processes for producing high quality, large-scale graphene is necessary for such applications to be enabled. Large area growth of graphene on the Si-terminated face of hexagonal SiC wafers exhibits manageable growth kinetics – contrary to the C-face – allowing good control over the number of graphene layers. Most importantly, the azimuthal orientation of epi-graphene on the Si-face of a SiC wafer is fixed. Therefore, it is a viable method for producing graphene with uniform coverage and structural coherence at wafer-scale.

Graphene was grown on SiC with two methods: i) By combining SiC surface preparation steps in disilane/He with a higher temperature (T=1550 °C) graphenization step in Ar and ii) By H2-etching SiC wafers at T>1500 °C to produce a vicinal, defect-free surface and then annealing that surface at T~1575 °C in Ar atmosphere (P~ 100 mbar).

After optimizing the process parameters for graphene growth on 4H(0001) SiC with 0.00° miscut, we have measured average Hall mobilities  up to 4900 cm2 V-1 s- 1 at sheet carrier densities N ~ 4x1011 cm-2 after a long exposure to ambient atmosphere. This mobility is higher and the electron density lower than the freshly made devices. The strong n-type character of pristine graphene on SiC (0001) is due to the dangling bonds below the  reconstruction (buffer layer), which act as positively charged traps. The reduction in N by ambient exposure is linked to the oxygen and water adsorbed onto the graphene surface. We can explain the large improvement in mobility with reduced N by taking into account several factors, including long-range Coulomb scattering and short-range scattering. A plot of  vs. N will be introduced as a benchmark of epi-graphene quality. After H2 intercalation, our epi-graphene becomes p-type and exhibits a record combination of high mobility and high hole density (far above the benchmark curve).

Support by DARPA Contracts FA8650-08-C-7838 & HR0011-12-C-0038 is gratefully acknowledged.