Role of C2H4 during CH4 Conversion to Benzene by

Supported MoOx/ZSM-5 Catalysts

Chris Walker, Yadan Tang and Israel E. Wachs

Department of Chemical and Biochemical Engineering

Lehigh University

Bethlehem, PA 18015 USA

The recent discovery of significant reserves of shale gas has triggered interest in gas-to-liquid technology (GTL) and especially a one-step process to convert methane to liquid hydrocarbon fuels. Methane dehydroaromatization (DHA) to benzene by supported MoOx/ZSM-5 catalysts has generated much interest. Despite extensive studies on this catalytic reaction system, debate remains about the reaction mechanism, catalytic functions of Mo and ZSM-5 support, and the rate-limiting step. This work aims to provide fundamental insights into these issues via CH4 and C2H4 temperature programmed surface reaction (TPSR) spectroscopy.

The CH4-TPSR measurements revealed that initiation of benzene formation requires ~700 oC and only with MoO3/ZSM-5 catalysts, while Mo-free HZSM-5 does not activate CH4. C2H4 is observed as a reaction intermediate during CH4 conversion to benzene. Corresponding C2H4-TPSR experiments demonstrated that C2H4 also produces benzene, but at much lower temperatures (~500 oC) and. These observations lead to the conclusions that the

- higher reaction temperature of CH4-TPSR demonstrates that methane C-H bond cleavage is the rate-limiting-step,

- activation of CH4 requires Mo sites,

- conversion of C2H4 to C6H6 does not require Mo sites and is catalyzed by Brønsted acid sites of the ZSM-5 support, and

- Mo sites increase the yield of benzene and decreases the activation temperature.

The presence of surface Mo sites on the ZSM-5 support decreases the amount of Brønsted acid sites and the moderate concentration of Brønsted acid sites for supported MoO3/ZSM-5 catalysts might suppress severe coking in comparison to Mo-free HZSM-5.