Fabrication of Non-Wetting Copper Surface via Solution Immersion Process

John B. Votaw, Won Tae Choi, Dennis W. Hess

School of Chemical & Biomolecular Engineering, Georgia Institute of Technology, Atlanta

Strongly liquid-repelling materials are of significant interest to many industries and scientific communities for the unique anti-fouling, contamination-resisting, and self-cleaning properties. Generally, metals exhibit a number of favorable properties, such as their malleability, ductility, and electrical conductivity. By creating a liquid-repelling metal surface, a technologically useful material with a combination of these unique properties can be formed. In this work, we discuss a method to control the surface topography of copper by chemical treatment. Control of the copper surface topography was achieved by immersion of copper foil into a solution of hydrochloric acid and hydrogen peroxide. Variation of the immersion time and temperature in the solution allowed further control over the copper foil topography:  by increasing either variable, there is an increase in pit density in the copper surface, which was confirmed by scanning electron microscopy.  A fluorocarbon film was then plasma-deposited onto the copper foil to modify the surface chemistry. When the appropriate combination of surface chemistry and topography were achieved, a strongly liquid-repelling copper surface was formed. The contact angles of water and hexadecane on these surfaces were as high as 166.2° and 104.3° respectively.