Facile One-Step Modification of Membrane Surface Using Zwitterionic Polymers for Wastewater Treatment

Nima Shahkaramipour, Sankara Narayanan Ramanan, Cheng Kee Lai, Chong Cheng, and Haiqing Lin*

Department of Chemical and Biological Engineering, University at Buffalo, The State University of New York, Buffalo, NY 14260, USA

* Corresponding author. Tel: +1-716-645-1856, Email: haiqingl@buffalo.edu (H. Lin)

Abstract

Polymeric membranes have been widely used for wastewater treatment. However, the membranes can be fouled by suspended solids and dissolved organic matters presented in the water, which block the membrane pores on the surface or inside the supports and thus decrease the water flux. Surface modification to enhance the hydrophilicity has been touted as a promising approach to reduce the fouling. In this study, we have modified ultrafiltration (UF) membranes using superhydrophilic zwitterionic polymers by facile one-step coating on the surface, aiming to reduce the fouling. More specifically, three commercial UF membranes, PES-2, PAN-50, and PS-100 are coated with a solution containing polydopamine (PDA) and sulfobetaine methacrylate (SBMA). The PDA and SBMA react and form a thin film on the surface, while PDA provides adhesion to the membrane surface and SBMA provides superhydrophilic properties. The coating enhances the surface hydrophilicity, which is confirmed by contact angle measurement. The effect of coating time and composition of the coating solutions on the water flux in the membranes is investigated. The membranes coated with zwitterionic materials (PDA+SBMA) demonstrate better stability and higher water flux than those of PDA coated and uncoated ones, when tested with wastewater containing bovine serum albumin (BSA) using a crossflow system. For instance, the modified PES-2, PAN-50, and PS-100 with PDA and SBMA, increased the water permeance by 65%, 81%, and 61%, respectively, compared to analogous uncoated membranes, after 3 hour filtration using a 3g/l BSA solution.