One-step synthesis of hybrid zeolite membranes containing catalytic metal nanoclusters

Seok-Jhin Kim, Shuai Tan, Micaela Taborga, Laura Briones Gil, David S. Sholl,

Christopher W. Jones, and Sankar Nair*

School of Chemical & Biomolecular Engineering, Georgia Institute of Technology,

Atlanta, GA 30332

Yujun Liu, Jason S. Moore, Ravindra S. Dixit, and John G. Pendergast Jr.

Engineering & Process Sciences, Core R&D, The Dow Chemical Company, Freeport, TX 77541

Karren L. More

Center for Nanophase Materials Sciences, Oak Ridge National Laboratory, Oak Ridge, TN 37831

ABSTRACT

Metal-loaded zeolitic membranes have promising applications as catalytic membranes that function simultaneously as reactors and separation devices. Post-treatment methods such as impregnation and ion exchange of metals need at least two or three steps, which increase the membrane production cost. Recent research has shown that a one-step synthesis method to encapsulate metal nanoparticles in zeolite powders offers a promising alternative to greatly improve the synthesis efficiency. However, to the best of our knowledge, the use of a one-step synthesis of zeolite membranes containing metal clusters has not yet been described in the literature.

We will discuss a one-step synthesis method to incorporate metal nanoparticles in zeolite membranes. The hybrid metal-zeolite membranes were prepared by one-step colloidal hydrothermal synthesis with addition of 3-mercaptopropyl-trimethoxysilane (MPS) and a metal precursor to the initial synthesis mixture. We show that Pt ions/clusters are uniformly distributed along the membrane cross sectional layer. High magnification scanning transmission electron microscopy (STEM) shows that the Pt metal clusters in the hybrid zeolite membrane have a narrow size distribution of 0.5-2.0 nm. In contrast, a pure-silica MFI membrane obtained from MPS-free precursor, shows negligible loading of Pt metal clusters throughout the zeolite membrane layer. We then show that hybrid metal-zeolite membranes can be used as catalytic membrane reactors (CMR) to investigate a high-temperature propane dehydrogenation (PDH) at 600 °C and 1 atm. The results indicate that Pt metal clusters formed within hybrid MFI zeolite membrane provide effective catalysts for high-temperature PDH reaction along with successful H2 removal through the membrane permeation. The hybrid zeolite MR was further tested for high-temperature PDH reaction at extended operating times, and showed excellent stability in performance.

*Corresponding author: E-mail: sankar.nair@chbe.gatech.edu