Zeolitic-Imidazolate Framework ZIF-8 Membranes Supported on Polymer Hollow Fibers Substrate for Propylene/Propane Separation

Mohamad Rezi Abdul Hamid1, Moon Joo Lee1, Jongmyeong Lee3, Ju Sung Kim3, Young Moo Lee3, and Hae-Kwon Jeong*1,2

1Artie McFerrin Department of Chemical Engineering and 2Department of Materials Science and Engineering, Texas A&M University, College Station, TX 77843-3122
3Department of Energy Engineering, College of Engineering, Hanyang University, Seoul 133-791, Republic of Korea

* Corresponding author: hjeong7@tamu.edu

Separation of olefin/paraffin mixtures (e.g., ethylene/ethane and propylene/propane), is one of the most challenging separations due to the similarity of their physicochemical properties. Currently, propylene/propane separation is typically achieved through cryogenic distillation, which are energy-intensive processes. Though energy-efficient membrane-based separation processes have drawn tremendous interest, however, there are no commercially available membranes for olefin/paraffin separations mainly due to the limitations of current membrane materials and lack of processing methods to fabricate large membranes area1-3.

A sub-class of metal-organic frameworks (MOFs), zeolitic-imidazolate frameworks (ZIFs) with zeolite topologies are crystalline nanoporous materials with well-defined aperture sizes (< 5 Å). ZIFs, which are composed of divalent metal ions (typically Zn2+ and Co2+) and imidazole-based organic linkers4 have been extensively studied for gas separation applications. ZIF-8 in particular is a promising membrane material for high resolution propylene/propane separation because the effective pore size of ZIF-8 (~ 4 Å) lies in between the size of propylene and propane molecules. While several ZIF-8 membranes on planar support showed high propylene/propane separation performances, scaling-up and commercialization of the membranes requires them to be fabricated on a cheap and scalable support (i.e., hollow fiber or tubular support). Polymeric hollow fibers have been utilized as substrates, but only a few of the resulting ZIF-8 membranes showed promising propylene/propane separation performances.6-9

Herein, we would like to present a microwave-microfluidic-based method to prepare well inter-grown ZIF-8 membranes on polymeric hollow fiber substrates. The method is modified based on our previously reported microwave-assisted seeding and secondary growth technique10. High-quality nano-sized ZIF-8 seed crystals were rapidly prepared on either inner or outer surface of hollow fibers under microwave heating. Subsequently, seed crystals were secondarily grown into continuous ZIF-8 films on polyimide hollow fibers. The thickness of the resulting ZIF-8 membranes were ~ 800 nm, one of the thinnest ZIF-8 membranes supported on polymer hollow fibers. The effects of different synthesis parameters on the microstructures of ZIF-8 membranes will be discussed. Finally, the gas separation performances of ZIF-8 membranes will be presented.

References and Notes

1 Koros, William J. and Fleming, G.K. (1993) “Membrane-based gas separation”, Journal of Membrane Science, 83, pp l-39

2 Baker RW., (2002) “Future Directions of Membrane Gas Separation Technology” Industrial & Engineering Chemistry Research., 41 (6), pp 1393-1411

3 Tanaka, K., Taguchi, A., Hao, JQ, Kita, H., and Okamoto, K., (1996) “Permeation and separation properties of polyimide membranes to olefins and paraffins”, Journal of Membrane Science, 121, pp 197-207

4 Park KS, Ni Z, Côté AP, et al., (2006) “Exceptional chemical and thermal stability of zeolitic imidazolate frameworks”, Proceedings of the National Academy of Sciences, 103 (27), pp 10186-10191

5 Zhang C, Lively RP, Zhang K, Johnson JR, Karvan O, Koros WJ., (2012) “Unexpected Molecular Sieving Properties of Zeolitic Imidazolate Framework-8”, The Journal of Physical Chemistry Letters., 3 (16), pp 2130-2134.

6 Andrew J. Brown, Nicholas A. Brunelli, Kiwon Eum, Fereshteh Rashidi, J. R. Johnson, William J. Koros, Christopher W. Jones, Sankar Nair, (2014) “Interfacial microfluidic processing of metal-organic framework hollow fiber membranes”, Science, 345, 6192, pp 72-75

7 FernandoCacho-Bailo, SilviaCatalán-Aguirre, MirenEtxeberría-Benavides, Oğuz Karvan, VictorSebastian, CarlosTéllez, JoaquínCoronas (2015) “Metal-organic framework membranes on the inner-side of a polymeric hollow fiber by microfluidic synthesis”, Journal of membrane science, 476, pp 277-285

8 Kiwon Eum, Chen Ma, Ali Rownaghi, Christopher W. Jones, and Sankar Nair (2016) “ZIF‑8 Membranes via Interfacial Microfluidic Processing in Polymeric Hollow Fibers: Efficient Propylene Separation at Elevated Pressures”, ACS Applied materials and interfaces, 8, pp 25337 – 25342

9 Anne M. Marti, Wasala Wickramanayake, Ganpat Dahe, Ali Sekizkardes, Tracy L. Bank, David P. Hopkinson, and Surendar R. Venna (2017) “Continuous Flow Processing of ZIF‑8 Membranes on Polymeric Porous Hollow Fiber Supports for CO2 Capture”, ACS Applied materials and interfaces, 9, pp 5678-5682

10 Kwon HT, Jeong H-K., (2013), “Highly propylene-selective supported zeolite-imidazolate framework (ZIF-8) membranes synthesized by rapid microwave-assisted seeding and secondary growth”, Chemical Communications, 49, pp 3854-3856