A new generation of inorganic/organic polymeric interfacial diffusion membranes is presented that have unprecedented combinations of high selectivity and flux. The membranes consist of an inorganic skaffold, with pores that are filled with a thermoplastic polymer that crystallizes in the pore space while a nm thin interfacial area remains amorphous. This special structure is thought to be promoted by the 10...100 nm scaffold pores and the inorganic surface. Selective molecular transport is blocked in the crystalline areas and takes place exclusively in the amorphous interfacial area. It is governed by a combination of affinity, mobility and size-exclusion. In the work presented the scaffold is made of pure α-Al2O3 with a porosity of ~30%, a surface pore size of 40 nm, and 100 nm otherwise. The polymer is polyether imide, present on top of the scaffold as a 1…3 μm amorphous layer, and inside the near-surface area of the scaffold over <1 μm. Combinations of extremely high gas selectivities were found of >2200 for CO2/N2 and >4000 for H2/N2, combined with permeances of 2.2 and 4.0×10–10 mol m–2 s–1 Pa–1, respectively. Conservative estimates of the membranes’ permeability indicate that their properties by far exceed the Robeson boundary, a well-known off-set between selectivity and permeability for organic polymeric membranes.