## Slide 1: Comparing Indigenous Laterite and Bauxite with Imported Activated Alumina for use in Small-scale Fluoride Adsorption Filters in Rural Northern Ghana
Laura Craig1, Lisa L. Stillings2, David L. Decker1, Jim M. Thomas1
1. Desert Research Institute and University of Nevada, Reno; 2. U.S. Geological Survey, Reno, NV

## Slide 2: Acknowledgments
University of Nevada, Reno
Desert Research Institute, Reno, NV
U.S. EPA STAR Graduate Research Fellowship
Geological Society of America Graduate Student Research Grant

## Slide 3: Presentation Outline
Describe study area in northern Ghana and problem - fluorosis
Possible solution - fluoride (F-) adsorption filters
Compare F- adsorption: Ghana bauxite and Namoo laterite (study area) to imported synthetic activated alumina
Physical and chemical properties controlling F- adsorption
Improve F- adsorption capacity of Ghana bauxite and Namoo laterite
Pros and cons of each sorbent for de-fluoridation filters in Ghana
Conclusions

## Slide 4: Study Area – Northern Ghana
Rural, poor - groundwater as primary water source
24 of 58 wells have F- above WHO limit of 1.5 ppm (mg/L)
Result – dental fluorosis (picture), risk of skeletal fluorosis
High F- GW
Low F- GW
Granite
(F- source)
< 1 ppm F-
2-4.6 ppm F-
Dental Fluorosis

## Slide 5: One Solution? Adsorption Filters at High F- Hand-pump Wells
Testing fluoride adsorption filter at hand-pump well, World Vision Ghana
Collect treated water
Hand-pump well
Two bins with sorbent

## Slide 6: Compare F- Loading: % F- Adsorption vs. F- Concentration
pHo ~ 6.9, I = 0.01 M, grain size = 0.5-1.0 mm
Chart: Initial mg F Soln/L
| 0.39 | 0.9 | 1.89 | 5.0599999999999996 | 10.029999999999999 | 19.8 | 26.27 | 39.43
Laterite | 10.2564 | 14.4444 | 13.7566 | 7.5099 | 9.0728 | 5.6061 | 5.7861 | 4.8694
Bauxite | 42.1053 | 41.6667 | 25.5319 | 18.1818 | 11.8782 | 7.6385 | 6.2708
Act Alum | 91.1111 | 95.8763 | 97.619 | 96.7546 | 91.9436 | 82.953 | 74.1709 | 65.4604 | 58.2641 | 55.1249 | 50.1259 | 43.9653 | 39.0958
GW F- range
Possible Ghanaian sorbents:
Namoo laterite (in study area)
Bauxite (western Ghana)
compared to
activated alumina (imported)

## Slide 7: Physical and Chemical Properties of Sorbents
*Surface area at grain size 0.5 to 1.0 mm
**Permanent charge not included
< pHPZNPC <
S - is sorbent surface:
Sorbent | Surf. Area* (m2 g-1) | pHPZNPC | %Al2O3 | %Fe2O3 | %SiO2
Act. alum. | 288.9 | 8.3 | 99.4 | 0.0 | 0.0
Gh. bauxite | 5.5 | 7.1** | 70.9 | 23.6 | 2.2
N. laterite | 21.9 | 7.3** | 13.5 | 36.8 | 45.7
Chart: I = 0.01 M
| -4.9237280865168362E-7 | -4.6201180291866347E-7 | -4.9084628757124686E-7 | -4.364896289763061E-7 | -3.834171400408438E-7 | -3.249522046234387E-7 | -2.6777377861723504E-7 | -2.3186975547433939E-7 | -1.7434240330731784E-7 | -1.181193306094512E-7 | -9.0540229848840448E-8 | -5.8466528628968608E-8 | -2.8056817869303421E-8 | 0 | 3.7909343042057964E-8 | 6.9467949380178652E-8 | 9.7880166370140924E-8 | 1.2121228134470988E-7 | 1.4986404331357704E-7 | 1.7733769062114126E-7 | 1.9251651015348877E-7 | 2.1361704026225047E-7 | 2.2606425382329217E-7 | 2.3835582194046296E-7 | 2.538194087353425E-7 | 2.7963066018579137E-7 | 3.0508451347647344E-7
Laterite | 9.97 | 9.93 | 9.83 | 9.75 | 9.65 | 9.53 | 9.36 | 9.19 | 9.05 | 8.83 | 8.68 | 8.54 | 8.28 | 7.3 | 6.33 | 5.73 | 5.43 | 5.2 | 4.83 | 4.63 | 4.47 | 4.3 | 4.17 | 4.07 | 4.02 | 4.01 | 4
Bauxite | 10 | 9.98 | 9.93 | 9.84 | 9.74 | 9.61 | 9.45 | 9.32 | 9.16 | 8.95 | 8.85 | 8.73 | 8.57 | 8.36 | 8.03 | 7.1 | 6.14 | 5.56 | 5.22 | 5.01 | 4.86 | 4.61 | 4.46 | 4.35 | 4.21 | 4.11 | 4.02
<------pHPZNPC

## Slide 8: Improving Adsorption: % F- Adsorption vs. pH
Chart: pH
| 3.4350000000000001 | 3.8800000000000003 | 4.4800000000000004 | 5.2799999999999994 | 6.09 | 6.52 | 6.71 | 7.6050000000000004 | 8.81 | 9.375 | 9.6266666666666669 | 9.870000000000001
Laterite | 54.35 | 46.4333 | 37.9 | 25.6 | 14.9 | 11.7 | 7.8 | 2.75 | 2.4333 | 1.6 | 2.6 | 1.55
Bauxite | 46.5 | 46.7 | 44.9 | 46.7 | 39.8 | 19.9 | 12.1 | 8.9 | 8.9 | 3.2 | 4 | 5.1 | 3.6 | 2.8 | 0.8
Act Alum | 81.9 | 81.2 | 79.8 | 77.9 | 86.4 | 99.3 | 99.02 | 91.7 | 85.3 | 79.3 | 73.7 | 69.3 | 57.3 | 52 | 48.8 | 47.9
Fluoride Adsorption Reactions
=
(S - is sorbent surface)
pH range of groundwater
G. Bauxite
N. Laterite
Fo = 10 mg/L, I = 0.01 M, 6.67 g/L

## Slide 9: Improving Adsorption: F- Adsorption vs. Grain Size
Namoo Laterite
Ghana Bauxite
Chart: Fo = 10 ppm, I = 0.01 M, 6.67 g/L
| 3.4350000000000001 | 3.8800000000000003 | 4.4800000000000004 | 5.2799999999999994 | 6.09 | 6.52 | 6.71 | 7.6050000000000004 | 8.81 | 9.375 | 9.6266666666666669 | 9.870000000000001
0.5-1.0 mm | 54.35 | 46.4333 | 37.9 | 25.6 | 14.9 | 11.7 | 7.8 | 2.75 | 2.4333 | 1.6 | 2.6 | 1.55
0.063-0.125 mm | 66 | 61 | 59.1 | 44.6 | 21 | 15.8 | 20.2 | 9.1 | 8.8 | 9.9 | 6.6 | 5.8 | 3.1 | 3.5 | 3.9
Chart: Fo = 10 ppm, I = 0.01 M, 6.67 g/L
| 3.43 | 3.63 | 4.24 | 5.35 | 5.69 | 6.05 | 6.29 | 6.87 | 7.39 | 8.4700000000000006 | 8.32 | 8.68 | 8.98 | 9.33 | 10
0.5-1.0 mm | 46.5 | 46.7 | 44.9 | 46.7 | 39.8 | 19.9 | 12.1 | 8.9 | 8.9 | 3.2 | 4 | 5.1 | 3.6 | 2.8 | 0.8
0.063-0.125 mm | 54 | 53.6 | 54.6 | 54.4 | 42.5 | 22.9 | 8.8 | 5.5 | 3.2 | 3.9 | 2.8 | 7.3
Adsorption improves with: (1) decreased pH (N. laterite < 4.5, G. bauxite < 6)
(2) decreased grain size (above)
(Note: activated alumina no increase in adsorption/surface area at 0.125 mm grain size)

## Slide 10: Pros and Cons Each Sorbent
Activated Alumina
Pros: high surface area & pHPZNPC ( surf. OH sites), Al2O3 = good F- sorbent
Cons: cost, imported
Ghana Bauxite
Pros: available in Ghana, mostly Al2O3 & Fe2O3 = good F- sorbent
Cons: low surface area, not available in north (must be transported)
Namoo Laterite
Pros: abundant in study area (no cost), ~50% Al2O3 & Fe2O3
Cons: contains a lot of quartz = adsorbs F- best low pH, moderately low
surface area

## Slide 11: Conclusions
Laterite and bauxite are not comparable to activated alumina as F- sorbent – but can be improved:
Much finer grain size will increase surface area and number of sorption sites for bauxite and laterite – feasible
Dropping pH of treatment water will increase F- adsorption of bauxite (pH<6) and laterite (pH<4.5) – less practical at small-scale
Additional long-term solutions?
* Large-scale drinking water treatment and distribution
* Find another water source (i.e. low F- piped water, rainwater)
* Health education – awareness of cause of fluorosis
Greater priorities in study area: jobs and improved access to water

## Slide 12
Questions? Comments?